Caledonian Mining Cables

AS/NZS 1802:2003 Reeling & Trailing Cables

Type 241 Superflex 1.1 to 6.6KV

» Applications .............................................................................................................

These cables are similar to Type 241 cables, except more flexible and have a smaller ‘natural’ bending radius, suitable for use as monorail cable where cable loops will be narrower, thus allowing more space for other equipment and reducing opportunities for getting snagged.

» Standards .................................................................................................................

AS/NZS 1802:2003

AS/NZS 1125

AS/NZS 3808

AS/NZS 5000.1

» Construction ............................................................................................................

Semiconductive PCP Filling And Covering Reinforcement

Stranded Tinned Copper Conductor

Conductor Screen Cradle Separator Central Extensible Pilot EPR Insulation Insulation Screen  Earth Conductor

Heavy Duty PCP Sheath

3×Conductors: Flexible stranded tinned annealed copper conductor.

Conductor Screen: Semiconductive compound (for cables having a voltage rating of 3.3/3.3kV and above).

Insulation: EPR.

Insulation Screen: Semiconductive elastomer.

Cradle Separator: Semiconductive PCP.

Overall Core Screen: Semiconductive PCP filling and covering.

3×Interstitial Earth Conductor: Semiconductive PCP covered flexible stranded tinned copper conductor.

1×Central Extensible Pilot: EPR covered flexible stranded tinned copper conductor.

Textile Reinforcement: Open-weave braid reinforcement.

16	www.caledonian-cables.co.uk  www.addison-cables.com

Caledonian Mining Cables

AS/NZS 1802:2003 Reeling & Trailing Cables

Sheath: Heavy duty PCP sheath. Heavy duty CPE/CSP sheath can be oﬀered upon request.

»  Dimensions and Weight ..........................................................................................

| Nominal Conductor Area | Strand Size | Insulation Thickness | Earth Conductor |  | Pilot Conductor |  | Thickness of Sheath Including SC PCP Layer | Nominal Overall Diameter | Nominal Weight |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Strand Size | Thickness of Covering | Strand Size | Thickness of Covering |  |  |  |
| mm² | No/mm | mm | No/mm | mm | No/mm | mm | mm | mm | kg/100m |
| Type 241.1 |  |  |  |  |  |  |  |  |  |
| 70 | 361/0.50 | 1.8 | 110/0.40 | 1.0 | 40/0.20 | 0.8 | 5.3 | 53.0 | 485 |
| 95 | 475/0.50 | 2.0 | 85/0.40 | 1.0 | 40/0.20 | 0.8 | 5.8 | 58.8 | 595 |
| 120 | 608/0.50 | 2.1 | 110/0.40 | 1.2 | 40/0.20 | 0.8 | 6.3 | 62.5 | 715 |
| 150 | 740/0.50 | 2.3 | 135/0.40 | 1.2 | 40/0.20 | 0.8 | 6.7 | 67.0 | 840 |
| 185 | 925/0.50 | 2.5 | 165/0.40 | 1.4 | 40/0.20 | 0.8 | 7.3 | 75.1 | 1040 |
| 240 | 1221/0.50 | 2.8 | 216/0.40 | 1.4 | 40/0.20 | 0.8 | 8.0 | 85.7 | 1340 |
| Type 241.3 |  |  |  |  |  |  |  |  |  |
| 70 | 361/0.50 | 3.0 | 110/0.40 | 1.2 | 40/0.20 | 0.8 | 6.4 | 61.2 | 590 |
| 95 | 475/0.50 | 3.0 | 135/0.40 | 1.2 | 40/0.20 | 0.8 | 6.8 | 65.9 | 710 |
| 120 | 608/0.50 | 3.0 | 165/0.40 | 1.2 | 40/0.20 | 0.8 | 7.2 | 68.9 | 820 |
| 150 | 740/0.50 | 3.0 | 216/0.40 | 1.2 | 40/0.20 | 0.8 | 7.6 | 72.5 | 940 |
| 185 | 925/0.50 | 3.0 | 252/0.40 | 1.4 | 40/0.20 | 0.8 | 8.0 | 79.4 | 1130 |
| 240 | 1221/0.50 | 3.0 | 324/0.40 | 1.4 | 40/0.20 | 0.8 | 8.6 | 88.3 | 1420 |
| Type 241.6 |  |  |  |  |  |  |  |  |  |
| 70 | 361/0.50 | 5.0 | 110/0.40 | 1.4 | 40/0.20 | 0.8 | 7.4 | 72.1 | 750 |
| 95 | 475/0.50 | 5.0 | 135/0.40 | 1.4 | 40/0.20 | 0.8 | 7.9 | 77.0 | 885 |
| 120 | 608/0.50 | 5.0 | 165/0.40 | 1.4 | 40/0.20 | 0.8 | 8.3 | 79.9 | 1000 |
| 150 | 740/0.50 | 5.0 | 216/0.40 | 1.4 | 40/0.20 | 0.8 | 8.6 | 83.3 | 1130 |
| 185 | 925/0.50 | 5.0 | 252/0.40 | 1.4 | 40/0.20 | 0.8 | 9.0 | 90.2 | 1330 |
| 240 | 1221/0.50 | 5.0 | 324/0.40 | 1.4 | 40/0.20 | 0.8 | 9.6 | 99.1 | 1640 |

www.caledonian-cables.co.uk  www.addison-cables.com	17