Caledonian Mining Cables

AS/NZS 1802:2003 Reeling & Trailing Cables

Type 245 1.1 to 6.6KV

» Applications .............................................................................................................

These very flexible cables are mainly used as longwall shearer cables, and also for continuous miners and peripheral longwall cables. Cable has 3 central pilots for earth continuity monitoring and for control circuits.

» Standards .................................................................................................................

AS/NZS 1802:2003

AS/NZS 1125

AS/NZS 3808

AS/NZS 5000.1

» Construction ............................................................................................................

Semiconductive PCP Filling And Covering Reinforcement

Stranded Tinned Copper Conductor

Conductor Screen Cradle Separator

Central Extensible Pilot/Control EPR Insulation

Insulation Screen Earth Conductor

Heavy Duty PCP Sheath

3×Conductors: Flexible stranded tinned annealed copper conductor.

Conductor Screen: Semiconductive compound (for cables having a voltage rating of 3.3/3.3kV and above).

Insulation: EPR.

Insulation Screen: Semiconductive elastomer.

Cradle Separator: Semiconductive PCP.

Overall Core Screen: Semiconductive PCP filling and covering.

3×Interstitial Earth Conductor: Semiconductive PCP covered flexible stranded tinned copper conductor.

3×Central Extensible Pilot: EPR covered flexible stranded tinned copper conductor.

Textile Reinforcement: Open-weave braid reinforcement.

Sheath: Heavy duty PCP sheath. Heavy duty CPE/CSP sheath can be oﬀered upon request.

18	www.caledonian-cables.co.uk  www.addison-cables.com

Caledonian Mining Cables

AS/NZS 1802:2003 Reeling & Trailing Cables

»  Dimensions and Weight ..........................................................................................

| Nominal Conductor Area | Strand Size | Insulation Thickness | Earth Conductor |  | Pilot Conductor |  | Thickness of Sheath Including SC PCP Layer | Nominal Overall Diameter | Nominal Weight |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Strand Size | Thickness of Covering | Strand Size | Thickness of Covering |  |  |  |
| mm² | No/mm | mm | No/mm | mm | No/mm | mm | mm | mm | kg/100m |
| Type 245.1 |  |  |  |  |  |  |  |  |  |
| 16 | 133/0.40 | 2.0 | 69/0.25 | 1.8 | 28/0.25 | 0.8 | 4.1 | 42.6 | 235 |
| 25 | 259/0.36 | 1.6 | 91/0.25 | 1.8 | 28/0.25 | 0.8 | 4.2 | 43.4 | 269 |
| 35 | 287/0.40 | 1.6 | 140/0.25 | 1.4 | 28/0.25 | 0.8 | 4.4 | 45.6 | 315 |
| 50 | 703/0.30 | 1.7 | 120/0.30 | 1.0 | 28/0.25 | 0.8 | 4.8 | 48.4 | 390 |
| 70 | 988/0.30 | 1.8 | 180/0.30 | 1.0 | 28/0.25 | 0.8 | 5.1 | 53.9 | 501 |
| 95 | 1332/0.30 | 2.0 | 150/0.30 | 1.0 | 28/0.25 | 0.8 | 5.6 | 60.4 | 630 |
| 120 | 1702/0.30 | 2.1 | 195/0.30 | 1.2 | 28/0.25 | 0.8 | 6.0 | 65.5 | 765 |
| 150 | 2146/0.30 | 2.3 | 235/0.30 | 1.2 | 28/0.25 | 0.8 | 6.3 | 70.5 | 915 |
| Type 245.3 |  |  |  |  |  |  |  |  |  |
| 25 | 259/0.36 | 3.0 | 91/0.25 | 1.5 | 28/0.25 | 0.8 | 5.2 | 51.1 | 338 |
| 35 | 287/0.40 | 3.0 | 140/0.25 | 1.0 | 28/0.25 | 0.8 | 5.4 | 54.5 | 398 |
| 50 | 703/0.30 | 3.0 | 120/0.30 | 1.0 | 28/0.25 | 0.8 | 5.7 | 56.8 | 490 |
| 70 | 988/0.30 | 3.0 | 180/0.30 | 1.2 | 28/0.25 | 0.8 | 6.0 | 61.2 | 592 |
| 95 | 1332/0.30 | 3.0 | 235/0.30 | 1.2 | 28/0.25 | 0.8 | 6.4 | 66.6 | 739 |
| 120 | 1702/0.30 | 3.0 | 300/0.30 | 1.2 | 28/0.25 | 0.8 | 6.7 | 71.0 | 870 |
| 150 | 2146/0.30 | 3.0 | 375/0.30 | 1.2 | 28/0.25 | 0.8 | 7.0 | 75.2 | 1028 |
| Type 245.6 |  |  |  |  |  |  |  |  |  |
| 50 | 703/0.30 | 5.0 | 120/0.30 | 1.4 | 28/0.25 | 0.8 | 6.7 | 67.2 | 635 |
| 70 | 988/0.30 | 5.0 | 180/0.30 | 1.4 | 28/0.25 | 0.8 | 7.0 | 71.7 | 755 |
| 95 | 1332/0.30 | 5.0 | 235/0.30 | 1.4 | 28/0.25 | 0.8 | 7.4 | 77.1 | 905 |
| 120 | 1702/0.30 | 5.0 | 300/0.30 | 1.4 | 28/0.25 | 0.8 | 7.7 | 81.3 | 1050 |
| 150 | 2146/0.30 | 5.0 | 375/0.30 | 1.4 | 28/0.25 | 0.8 | 8.0 | 85.8 | 1210 |

www.caledonian-cables.co.uk  www.addison-cables.com	19