Caledonian Mining Cables

Portable Power Cables

Type W Single Conductor Portable Power Cable 2kV

» Applications .............................................................................................................

These cables are designed for use on electric mining locomotives and other mobile equipment of the gathering-reel type, where the cable must withstand constant ﬂexing and reeling�

» Standards .................................................................................................................

ICEA S-75-381/NEMA WC 58 ASTM B 172

ASTM B 33

CAN/CSA C22�2 No� 96

» Construction ............................................................................................................

Stranded Tinned Copper Conductor

EPR Insulation

Reinforcement

CPE Jacket

Conductors:

Stranded annealed tinned copper conductor�

Insulation:

Ethylene Propylene Rubber (EPR)�

Reinforcement:

A layer of polyester braid, applied between the insulation and jacket for mechanical strength�

Jacket:

Heavy-duty/extra-heavy-duty Chlorinated Polyethylene (CPE), black� (Cables having a nominal outside diameter of more than 2�0 inches require extra-heavy-duty jackets�)

www.caledonian-cables.co.uk  www.addison-cables.com	1

Caledonian Mining Cables

Portable Power Cables

» Options .....................................................................................................................

- Other jacket materials such as CSP/PCP/NBR/PVC are available upon request�

- Two-layer jacket with reinforcing fibre between the two layers can be oﬀered  as an option�

»  Mechanical and Thermal Properties ......................................................................

Minimum Bending Radius: 6×OD

Maximum Conductor Operating Temperature: +90℃

»  Dimensions and Weight ..........................................................................................

| Construction | No. of Strands | Nominal Insulation Thickness |  | Nominal Jacket Thickness |  | Nominal Overall Diameter |  | Nominal Weight |  | Ampacity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No. of cores×AWG/kcmil | - | inch | mm | inch | mm | inch | mm | lbs/kft | kg/km | A |
| 1×8 | 133 | 0�060 | 1�5 | 0�060 | 1�5 | 0�44 | 11�2 | 150 | 223 | 83 |
| 1×6 | 168 | 0�060 | 1�5 | 0�080 | 2�0 | 0�51 | 13�0 | 205 | 305 | 109 |
| 1×4 | 259 | 0�060 | 1�5 | 0�080 | 2�0 | 0�57 | 14�5 | 280 | 417 | 145 |
| 1×3 | 329 | 0�060 | 1�5 | 0�095 | 2�4 | 0�63 | 16�0 | 350 | 521 | 167 |
| 1×2 | 259 | 0�060 | 1�5 | 0�095 | 2�4 | 0�66 | 16�8 | 370 | 550 | 192 |
| 1×1 | 329 | 0�080 | 2�0 | 0�110 | 2�8 | 0�74 | 18�8 | 500 | 744 | 223 |
| 1×1/0 | 259 | 0�080 | 2�0 | 0�110 | 2�8 | 0�77 | 19�6 | 550 | 818 | 258 |
| 1×2/0 | 329 | 0�080 | 2�0 | 0�110 | 2�8 | 0�82 | 20�1 | 660 | 982 | 298 |
| 1×3/0 | 427 | 0�080 | 2�0 | 0�125 | 3�2 | 0�87 | 22�1 | 830 | 1235 | 345 |
| 1×4/0 | 532 | 0�080 | 2�0 | 0�125 | 3�2 | 0�93 | 23�6 | 950 | 1413 | 400 |
| 1×250 | 608 | 0�095 | 2�4 | 0�140 | 3�6 | 1�03 | 26�2 | 1240 | 1845 | 445 |
| 1×300 | 741 | 0�095 | 2�4 | 0�140 | 3�6 | 1�09 | 27�7 | 1400 | 2083 | 500 |
| 1×350 | 855 | 0�095 | 2�4 | 0�155 | 3�9 | 1�15 | 29�2 | 1480 | 2202 | 552 |
| 1×500 | 1221 | 0�095 | 2�4 | 0�155 | 3�9 | 1�31 | 33�3 | 2140 | 3184 | 695 |

Ampacity-Based on a conductor temperature of 90℃ and an ambient air temperature of 40℃, per ICEA S-75-381�

2	www.caledonian-cables.co.uk  www.addison-cables.com