Caledonian Mining Cables

Portable Power Cables

Type G Four-Conductor Round Portable Power Cable 2kV

» Applications .............................................................................................................

These cables are designed for use with mobile mining equipment, such as continuous miners, cutting or loading machines, conveyors, drills or pumps�

»  Standards

................................................................................................................

ICEA S-75-381/NEMA WC 58 ASTM B 172

ASTM B 33

CAN/CSA C22�2 No� 96

» Construction ............................................................................................................

Stranded Tinned Copper Conductor EPR Insulation

Grounding Conductor Reinforced CPE Jacket

Conductors:

Stranded annealed tinned copper conductor�

Insulation:

Ethylene Propylene Rubber (EPR)�

Grounding Conductor:

Tinned copper conductor with an optional green outer covering�

Jacket:

Reinforced heavy-duty/extra-heavy-duty Chlorinated Polyethylene (CPE), black� (Cables having a nominal outside diameter of more than 2�0 inches require extra-heavy-duty jackets�)

www.caledonian-cables.co.uk  www.addison-cables.com	21

Caledonian Mining Cables

Portable Power Cables

» Options .....................................................................................................................

- Other jacket materials such as CSP/PCP/NBR/PVC are available upon request�

- Two-layer jacket with reinforcing fibre between the two layers can be oﬀered  as an option�

»  Mechanical and Thermal Properties ......................................................................

Minimum Bending Radius: 6×OD

Maximum Conductor Operating Temperature: +90℃

»  Dimensions and Weight

........................................................................................

| Construction | No. of Strands | Grounding Conductor Size | Nominal Insulation Thickness |  | Nominal Jacket Thickness |  | Nominal Overall Diameter |  | Nominal Weight |  | Ampacity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No. of cores×AWG/kcmil | - | AWG/ kcmil | inch | mm | inch | mm | inch | mm | lbs/kft | kg/km | A |
| 4×6 | 259 | 12 | 0�06 | 1�5 | 0�140 | 3�6 | 1�10 | 27�9 | 910 | 1354 | 72 |
| 4×4 | 412 | 10 | 0�06 | 1�5 | 0�155 | 3�9 | 1�27 | 32�3 | 1378 | 2050 | 93 |
| 4×2 | 259 | 9 | 0�06 | 1�5 | 0�170 | 4�3 | 1�48 | 37�6 | 1914 | 2848 | 122 |
| 4×1 | 331 | 8 | 0�08 | 2�0 | 0�190 | 4�8 | 1�68 | 42�7 | 2311 | 3438 | 143 |
| 4×1/0 | 414 | 7 | 0�08 | 2�0 | 0�190 | 4�8 | 1�79 | 45�5 | 2810 | 4181 | 165 |
| 4×2/0 | 522 | 6 | 0�08 | 2�0 | 0�190 | 4�8 | 1�93 | 49�0 | 3253 | 4840 | 192 |
| 4×3/0 | 658 | 5 | 0�08 | 2�0 | 0�205 | 5�2 | 2�07 | 52�6 | 4099 | 6099 | 221 |
| 4×4/0 | 829 | 4 | 0�08 | 2�0 | 0�220 | 5�6 | 2�26 | 57�4 | 4925 | 7327 | 255 |
| 4×250 | 973 | 3 | 0�095 | 2�4 | 0�235 | 6�0 | 2�66 | 67�6 | 6060 | 9016 | 280 |
| 4×350 | 1361 | 1 | 0�095 | 2�4 | 0�250 | 6�4 | 2�98 | 75�7 | 8126 | 12090 | 335 |
| 4×500 | 1921 | 1/0 | 0�095 | 2�4 | 0�280 | 7�1 | 3�40 | 86�4 | 10758 | 16006 | 395 |

Ampacity-Based on a conductor temperature of 90℃ and an ambient air temperature of 40℃, per ICEA S-75-381�

22	www.caledonian-cables.co.uk  www.addison-cables.com