Caledonian Mining Cables

Portable Power Cables

Type G-GC Three-Conductor Flat Portable Power Cable 2kV

» Applications .............................................................................................................

These flat parallel cables are designed for use on AC mining equipment, such as A�C� shuttle cars, drills, cutting and loading machines�

»  Standards

................................................................................................................

ICEA S-75-381/NEMA WC 58 ASTM B 172

ASTM B 33

CAN/CSA-C22�2 No�96

» Construction ............................................................................................................

Stranded Tinned Copper Conductor

Ground Check Conductor

Synthetic Yarn Braid Renforcement

CPE Jacket EPR Insulation

Grounding  Conductor

Conductors:

Stranded annealed tinned copper conductor�

Insulation:

Ethylene Propylene Rubber (EPR)�

Ground Check Conductor:

Tinned copper conductor with a yellow insulation�

Grounding Conductor:

Tinned copper conductor with an optional green outer covering�

Reinforcement:

Synthetic yarn�

www.caledonian-cables.co.uk  www.addison-cables.com	23

Caledonian Mining Cables

Portable Power Cables

Jacket:

Heavy-duty/extra-heavy-duty Chlorinated Polyethylene (CPE), black� (Cables having a nominal outside diameter of more than 2�0 inches require extra-heavy-duty jackets�)

» Options .....................................................................................................................

- Other jacket materials such as CSP/PCP/NBR/PVC are available upon request�

- Two-layer jacket with reinforcing fibre between the two layers can be oﬀered  as an option�

»  Mechanical and Thermal Properties ......................................................................

Minimum Bending Radius: 6×OD

Maximum Conductor Operating Temperature: +90℃

»  Dimensions and Weight

........................................................................................

| Construction | No. of Strands | Grounding Conductor Size | Ground Check Conductor Size | Nominal Insulation Thickness |  | Nominal Jacket Thickness |  | Nominal Overall Diameter Height×Width |  | Nominal Weight |  | Ampacity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No. of cores×AWG/ kcmil | - | AWG/ kcmil | AWG/ kcmil | inch | mm | inch | mm | inch | mm | lbs/kft | kg/km | A |
| 3×6 | 133 | 8 | 8 | 0�06 | 1�5 | 0�095 | 2�4 | 0�66×1�67 | 16�8×42�4 | 900 | 1340 | 79 |
| 3×4 | 259 | 7 | 8 | 0�06 | 1�5 | 0�095 | 2�4 | 0�72×1�87 | 18�3×47�5 | 1175 | 1750 | 104 |
| 3×3 | 259 | 6 | 6 | 0�06 | 1�5 | 0�110 | 2�8 | 0�78×2�08 | 19�8×52�8 | 1395 | 2080 | 120 |
| 3×2 | 259 | 5 | 6 | 0�06 | 1�5 | 0�110 | 2�8 | 0�85×2�23 | 21�6×56�6 | 1625 | 2415 | 138 |
| 3×1 | 259 | 4 | 6 | 0�08 | 2�0 | 0�125 | 3�2 | 0�96×2�50 | 24�4×63�5 | 2090 | 3110 | 161 |
| 3×1/0 | 259 | 3 | 5 | 0�08 | 2�0 | 0�140 | 3�6 | 1�01×2�67 | 25�6×67�8 | 2470 | 3675 | 186 |
| 3×2/0 | 329 | 2 | 5 | 0�08 | 2�0 | 0�140 | 3�6 | 1�09×2�86 | 27�7×68�1 | 2940 | 4375 | 215 |
| 3×3/0 | 413 | 1 | 5 | 0�08 | 2�0 | 0�155 | 3�9 | 1�18×3�12 | 30�0×79�2 | 3515 | 5230 | 249 |
| 3×4/0 | 532 | 1/0 | 5 | 0�08 | 2�0 | 0�155 | 3�9 | 1�24×3�30 | 31�5×83�8 | 4245 | 6315 | 287 |

Ampacity-Based on a conductor temperature of 90℃ and an ambient air temperature of 40℃, per ICEA S-75-381�

24	www.caledonian-cables.co.uk  www.addison-cables.com