Caledonian Mining Cables

Portable Power Cables

Type SHD-CGC Three-Conductor Round Portable Power Cable 2kV

» Applications .............................................................................................................

These heavy duty cables are designed for applications such as longwall shearers, continuous miners, loaders, drills, conveyors, pumps, and other mobile equipment requiring grounding conductors, where a ground check conductor, and metallic shielding are required�

»  Standards

................................................................................................................

ICEA S-75-381/NEMA WC 58 ASTM B 172

ASTM B 33

CAN/CSA C22�2 No� 96

» Construction ............................................................................................................

Stranded Tinned Copper Conductor

EPR Insulation

Ground Check Conductor

Insulation Shield

Grounding Conductor

Reinforced CPE Jacket

Conductors:

Stranded annealed tinned copper conductor�

Insulation:

Ethylene Propylene Rubber (EPR)�

Insulation Shield:

Tinned copper/textile braid�

Ground Check Conductor:

Tinned copper with a yellow insulation, located in the center of the cable�

www.caledonian-cables.co.uk  www.addison-cables.com	33

Caledonian Mining Cables

Portable Power Cables

Grounding  Conductor: Tinned copper conductor� Jacket:

Reinforced extra-heavy-duty Chlorinated Polyethylene (CPE), black�

» Options .....................................................................................................................

- Other jacket materials such as CSP/PCP/NBR/PVC are available upon request�

- Two-layer jacket with reinforcing fibre between the two layers can be oﬀered  as an option�

»  Mechanical and Thermal Properties ......................................................................

Minimum Bending Radius: 6×OD

Maximum Conductor Operating Temperature: +90℃

»  Dimensions and Weight

........................................................................................

| Construction | No. of Strands | Grounding Conductor Size | Ground Check Conductor Size | Nominal Insulation Thickness |  | Nominal Jacket Thickness |  | Nominal Overall Diameter |  | Nominal Weight |  | Ampacity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No. of cores×AWG/ kcmil | - | AWG/ kcmil | AWG/ kcmil | inch | mm | inch | mm | inch | mm | lbs/kft | kg/km | A |
| 3×2/0 | 342 | 5 | 16 | 0�08 | 2�0 | 0�205 | 5�2 | 2�09 | 53�1 | 3400 | 5059 | 243 |
| 3×3/0 | 418 | 4 | 16 | 0�08 | 2�0 | 0�205 | 5�2 | 2�21 | 56�1 | 3934 | 5853 | 279 |
| 3×4/0 | 532 | 3 | 16 | 0�08 | 2�0 | 0�220 | 5�6 | 2�36 | 59�9 | 4860 | 7231 | 321 |
| 3×350 | 888 | 1 | 16 | 0�95 | 2�4 | 0�250 | 6�3 | 2�81 | 71�4 | 7400 | 11010 | 435 |

Ampacity-Based on a conductor temperature of 90℃ and an ambient air temperature of 40℃, per ICEA S-75-381�

34	www.caledonian-cables.co.uk  www.addison-cables.com