Caledonian Mining Cables

Technical Information

Inuslation & Jacket Material Characteristics Comparison Chart

1=Poor, 2=Fair, 3=Good, 4=Very Good, 5=Excellent

| Chemical | Neoprene (PCP) | Chlorinated Sulfonated Polyethylene (CSP/CSPE ) | Chlorinated Polyethylene (CPE) | Polyurethane (PU) | Ethylene Propylene (EPR) | Polyvinyl Chloride (PVC) |
| --- | --- | --- | --- | --- | --- | --- |
| Acetic acid | 1 | 2 | 2 | 2 | 1 | 1 |
| Benzene | 2 | 2 | 2 | 1 | 1 | 2 |
| Bitumous tar | 3 | 3 | 3 | 3-4 | 1 | 3 |
| Bleach (NaCLO2) | 4 | 4 | 4 | 2 | 5 | 4 |
| Coke oven gas | 4 | 4 | 4 | 4 | 4 | 4 |
| Diesel oil | 2 | 4 | 4 | 4 | 2 | 4 |
| Ethylene glycol | 4 | 4 | 4 | 2 | 5 | 3 |
| Gasoline | 3 | 3 | 3 | 5 | 2 | 2 |
| Hydraulic oil | 4 | 4 | 4 | 5 | 1 | 4 |
| Hydrochloric acid (21%) | 5 | 5 | 5 | 2 | 1 | 4 |
| Hydrogen sulphide | 5 | 4 | 5 | 1 | 5 | 4 |
| Kerosene | 3 | 3 | 3 | 4 | 2 | 2 |
| Methanol | 5 | 5 | 5 | 2 | 5 | 3 |
| Methyl ethyl keton | 3 | 3 | 3 | 3 | 5 | 1 |
| Nitric acid (10%) | 3 | 5 | 5 | 2 | 5 | 4 |
| Phosphoric acid (60%) | 4 | 5 | 5 | 3 | 5 | 5 |
| Picric acid (10%) | 5 | 5 | 5 | 2 | 4 | 5 |
| Potassium chloride | 5 | 5 | 5 | 5 | 5 | 5 |
| Sodium hydroxide (25%) | 5 | 5 | 5 | 1 | 5 | 3 |
| Sulphuric acid (50%) | 5 | 5 | 5 | 1 | 5 | 4 |
| Transformer oil | 3-4 | 3 | 4 | 5 | 2 | 4 |
| Trichlorethylene | 1 | 1 | 1 | 1-2 | 1 | 1 |
| Vegetable oils & fats | 4 | 4 | 4 | 5 | 4 | 4 |
| UV resistance | 5 | 5 | 5 | 5 | 5 | 3 |
| Ozone resistance | 4 | 4-5 | 4-5 | 5 | 5 | 5 |
| Water resistance | 5 | 5 | 4 | 2 | 5 | 3 |
| Tear & notch resistance | 4-5 | 3 | 4 | 5 | 2-3 | 4 |
| Low temp. flexibility | 4-5 | 4 | 3 | 5 | 5 | 3 |
| Abrasion resistance | 4-5 | 4 | 3-4 | 5 | 3 | 4 |

88	www.caledonian-cables.co.uk  www.addison-cables.com