Caledonian Mining Cables

Portable Power Cables

Type W Four-Conductor Round Portable Power Cable 2kV

» Applications .............................................................................................................

These cables are designed for use with mobile mining equipment such as continuous miners, drills, cutters, loading machines and AC shuttle cars� Type W cables are for applications where bare grounding conductors are not required or desired�

» Standards .................................................................................................................

ICEA S-75-381/NEMA WC 58 ASTM B 172

ASTM B 33

CAN/CSA C22�2 No� 96

» Construction ............................................................................................................

Stranded Tinned Copper Conductor

EPR Insulation

Reinforced CPE Jacket

Conductors:

Stranded annealed tinned copper conductor�

Insulation:

Ethylene Propylene Rubber (EPR)�

Jacket:

Reinforced heavy-duty/extra-heavy-duty Chlorinated Polyethylene (CPE), black� (Cables having a nominal outside diameter of more than 2�0 inches require extra-heavy-duty jackets�)

www.caledonian-cables.co.uk  www.addison-cables.com	11

Caledonian Mining Cables

Portable Power Cables

» Options .....................................................................................................................

- Other jacket materials such as CSP/PCP/NBR/PVC are available upon request�

- Two-layer jacket with reinforcing fibre between the two layers can be oﬀered  as an option�

»  Mechanical and Thermal Properties ......................................................................

Minimum Bending Radius: 6×OD

Maximum Conductor Operating Temperature: +90℃

»  Dimensions and Weight ..........................................................................................

| Construction | No. of Strands | Nominal Insulation Thickness |  | Nominal Jacket Thickness |  | Nominal Overall Diameter |  | Nominal Weight |  | Ampacity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No. of cores×AWG/ kcmil | - | inch | mm | inch | mm | inch | mm | lbs/kft | kg/km | A |
| 4×8 | 133 | 0�06 | 1�5 | 0�125 | 3�2 | 0�99 | 25�2 | 670 | 997 | 54 |
| 4×6 | 133 | 0�06 | 1�5 | 0�140 | 3�6 | 1�10 | 27�9 | 838 | 1247 | 72 |
| 4×4 | 259 | 0�06 | 1�5 | 0�155 | 3�9 | 1�27 | 32�3 | 1174 | 1747 | 93 |
| 4×3 | 259 | 0�06 | 1�5 | 0�155 | 3�9 | 1�34 | 34�0 | 1377 | 2049 | 106 |
| 4×2 | 259 | 0�06 | 1�5 | 0�170 | 4�3 | 1�48 | 37�6 | 1701 | 2531 | 122 |
| 4×1 | 259 | 0�08 | 2�0 | 0�190 | 4�8 | 1�68 | 42�7 | 2192 | 3262 | 143 |
| 4×1/0 | 266 | 0�08 | 2�0 | 0�190 | 4�8 | 1�79 | 45�5 | 2549 | 3793 | 165 |
| 4×2/0 | 342 | 0�08 | 2�0 | 0�190 | 4�8 | 1�93 | 49�0 | 3078 | 4581 | 192 |
| 4×3/0 | 418 | 0�08 | 2�0 | 0�205 | 5�2 | 2�07 | 52�6 | 3685 | 5485 | 221 |
| 4×4/0 | 532 | 0�08 | 2�0 | 0�220 | 5�6 | 2�26 | 57�4 | 4540 | 6758 | 255 |
| 4×250 | 627 | 0�095 | 2�4 | 0�235 | 6�0 | 2�66 | 67�6 | 5746 | 8553 | 280 |
| 4×350 | 888 | 0�095 | 2�4 | 0�250 | 6�4 | 2�98 | 75�7 | 7574 | 11275 | 335 |
| 4×500 | 1221 | 0�095 | 2�4 | 0�280 | 7�1 | 3�40 | 86�4 | 10376 | 15441 | 395 |

Ampacity-Based on a conductor temperature of 90℃ and an ambient air temperature of 40℃, per ICEA S-75-381�

12	www.caledonian-cables.co.uk  www.addison-cables.com