Caledonian Mining Cables

Portable Power Cables

Type W Five-Conductor Round Portable Power Cable 2kV

» Applications .............................................................................................................

These cables are designed for use with mobile mining equipment such as continuous miners, drills, cutters, loading machines and AC shuttle cars� Type W cables are for applications where bare grounding conductors are not required or desired�

» Standards .................................................................................................................

ICEA S-75-381/NEMA WC 58 ASTM B 172

ASTM B 33

CAN/CSA C22�2 No� 96

» Construction ............................................................................................................

Stranded Tinned Copper Conductor

EPR Insulation

Reinforced CPE Jacket

Conductors:

Stranded annealed tinned copper conductor�

Insulation:

Ethylene Propylene Rubber (EPR)�

Jacket:

Reinforced heavy-duty/extra-heavy-duty Chlorinated Polyethylene (CPE), black� (Cables having a nominal outside diameter of more than 2�0 inches require extra-heavy-duty jackets�)

www.caledonian-cables.co.uk  www.addison-cables.com	13

Caledonian Mining Cables

Portable Power Cables

» Options .....................................................................................................................

- Other jacket materials such as CSP/PCP/NBR/PVC are available upon request�

- Two-layer jacket with reinforcing fibre between the two layers can be oﬀered  as an option�

»  Mechanical and Thermal Properties ......................................................................

Minimum Bending Radius: 6×OD

Maximum Conductor Operating Temperature: +90℃

»  Dimensions and Weight ..........................................................................................

| Construction | No. of Strands | Nominal Insulation Thickness |  | Nominal Jacket Thickness |  | Nominal Overall Diameter |  | Nominal Weight |  | Ampacity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No. of cores×AWG/kcmil | - | inch | mm | inch | mm | inch | mm | lbs/kft | kg/km | A |
| 5×8 | 133 | 0�06 | 1�5 | 0�140 | 3�6 | 1�07 | 27�2 | 776 | 1154 | 50 |
| 5×6 | 133 | 0�06 | 1�5 | 0�155 | 3�9 | 1�24 | 31�5 | 1024 | 1524 | 68 |
| 5×4 | 259 | 0�06 | 1�5 | 0�155 | 3�9 | 1�36 | 35�2 | 1432 | 2131 | 88 |
| 5×2 | 259 | 0�06 | 1�5 | 0�170 | 4�3 | 1�56 | 39�8 | 2051 | 3052 | 116 |
| 5×1 | 259 | 0�06 | 1�5 | 0�190 | 4�8 | 1�85 | 47�1 | 2665 | 3967 | 136 |
| 5×1/0 | 266 | 0�08 | 2�0 | 0�205 | 5�2 | 1�98 | 50�4 | 3406 | 5069 | 150 |
| 5×2/0 | 342 | 0�08 | 2�0 | 0�205 | 5�2 | 2�13 | 54�1 | 3596 | 5351 | 172 |
| 5×3/0 | 418 | 0�08 | 2�0 | 0�220 | 5�6 | 2�27 | 57�6 | 4728 | 7035 | 200 |
| 5×4/0 | 532 | 0�08 | 2�0 | 0�220 | 5�6 | 2�46 | 62�6 | 5512 | 8203 | 230 |

Ampacity-Based on a conductor temperature of 90℃ and an ambient air temperature of 40℃, per ICEA S-75-381�

14	www.caledonian-cables.co.uk  www.addison-cables.com