Caledonian Mining Cables Cables for Underground Mining

NTSCGERLWOEU 3.6/6kV Flexible Submersible Cable

»  Applications

These cables are used for permanent operation in water where the cable is required to have

additional mechanical protection.

»  Standards

VDE 0250 Part 813

»  Construction

Stranded Copper Conductor 3GI3 Rubber Insulation Optional Pilot Cores

Earth Conductor

Synthetic Butyl Rubber Inner Sheath Galvanised Steel Wire Braid

5GM5 Rubber Outer Sheath

Conductors: Flexible stranded tinned copper conductor, class 5 according to DIN VDE 0295.

Inner Conductor Layer: Special rubber compound, conductive.

Insulation: Rubber type 3GI3.

Outer Conductor Layer: Special rubber, conductive, easy strippable.

Pilot Cores (optional): Copper conductor with EPR insulation. Earth Conductor: Spiral of tinned annealed copper wires. Inner Sheath: Waterproof synthetic butyl rubber.

Armouring: Braid of galvanised steel strands.

Outer Sheath: Rubber type 5GM5.

www.caledonian-cables.co.uk  www.addison-cables.com	27

Caledonian Mining Cables

Cables for Underground Mining

»  Dimensions and Weight

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×35+3×16/3E | 55�0 | 60�0 | 4600 |
| 3×50+3×25/3E | 59�0 | 67�0 | 5600 |
| 3×70+3×35/3E | 64�0 | 70�0 | 6700 |
| 3×95+3×50/3E | 68�0 | 75�0 | 7900 |
| 3×120+3×70/3E | 75�0 | 80�0 | 9980 |

28	www.caledonian-cables.co.uk  www.addison-cables.com