Caledonian Mining Cables

Cables for Underground Mining

N3GHSSYCY Medium Voltage Cable

»  Applications

These cables are used for the connection of mobile operating equipment, in mines and underground excavations with hazardous environments, in stationary operation, e.g. high-voltage transformers in mining and tunnelling.

»  Standards

VDE 0250 Part 605

»  Construction

Monitoring Conductor PVC Intermediate Sheath Galvanized Steel Wires Braid 5GM5 Rubber Outer Sheath

Stranded Copper Conductor Pilot Cores

3GI3 Rubber Insulation Earth Conductor

PVC Inner Sheath

Conductors: Flexible stranded copper conductor, class 5 according to DIN VDE 0295.

Insulation: EPR compound type 3GI3.

Electrical Field Control: Inner and outer semiconductive layer of semiconductive rubber, for 6 kV outer semiconductive layer only.

Pilot Cores: Stranded copper conductor with EPR insulation.

Earth Conductor: Spiral of copper wires over the outer semi-conductive layer of the cores.

Inner Sheath: PVC compound type YM5.

Monitoring Conductor: Conductive tape serving and overall concentric Cu wire spinning.

Intermediate Sheath: PVC compound type YM5.

Armour: Braid of galvanized steel wires.

Outer Sheath: PVC compound type YM5.

38	www.caledonian-cables.co.uk  www.addison-cables.com

Caledonian Mining Cables Cables for Underground Mining

»  Dimensions and Weight

3.6/6kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+3×16/3E+3×2�5ST+UEL | 49�0 | 53�0 | 4190 |
| 3×35+3×16/3E+3×2�5ST+UEL | 52�0 | 56�0 | 4800 |
| 3×50+3×25/3E+3×2�5ST+UEL | 55�0 | 59�0 | 5600 |
| 3×70+3×35/3E+3×2�5ST+UEL | 59�0 | 63�0 | 6650 |
| 3×95+3×50/3E+3×2�5ST+UEL | 63�0 | 67�0 | 7940 |

6/10kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+3×16/3E+3×2�5ST+UEL | 55�0� | 58�0 | 5300 |
| 3×35+3×16/3E+3×2�5ST+UEL | 58�0 | 61�0 | 5910 |
| 3×50+3×25/3E+3×2�5ST+UEL | 61�0 | 65�0 | 6790 |
| 3×70+3×35/3E+3×2�5ST+UEL | 65�0 | 69�0 | 7860 |
| 3×95+3×50/3E+3×2�5ST+UEL | 68�0 | 73�0 | 9180 |

8.7/15kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+3×16/3E+3×2�5ST+UEL | 58�0 | 62�0 | 6810 |
| 3×35+3×16/3E+3×2�5ST+UEL | 61�0 | 65�0 | 7850 |
| 3×50+3×25/3E+3×2�5ST+UEL | 64�7 | 68�7 | 9130 |
| 3×70+3×35/3E+3×2�5ST+UEL | 67�9 | 71�9 | 10750 |
| 3×95+3×50/3E+3×2�5ST+UEL | 72�4 | 76�4 | 12290 |

12/20kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+3×16/3E+3×2�5ST+UEL | 62�3 | 66�3 | 8790 |
| 3×35+3×16/3E+3×2�5ST+UEL | 65�3 | 69�3 | 9930 |
| 3×50+3×25/3E+3×2�5ST+UEL | 69�0 | 73�0 | 11360 |
| 3×70+3×35/3E+3×2�5ST+UEL | 72�2 | 76�2 | 13100 |
| 3×95+3×50/3E+3×2�5ST+UEL | 76�8 | 80�8 | 14750 |

www.caledonian-cables.co.uk  www.addison-cables.com	39