(N)TSCGEWOEU Medium Voltage Fixed Installation Cable

With Fiber Optics

»  Applications

These cables are used for For laying alongside the conveyor belts (also for shiftable units) and on material handling equipment (even with continuous movement such as in cable booms or as connection between upper and lower car) and for connection of submersible pump units.

»  Standards

Based on VDE 0250 Part 813

»  Construction

Stranded Copper Conductor Fibre Optic Element

EPR Insulation EPR Inner Sheath Earth Conductor

CM Rubber Outer Sheath

Conductors: Flexible stranded copper conductor, class 5 according to DIN VDE 0295.

Inner Conductor Layer: Semiconductive layer.

Insulation: EPR.

Outer Conductor Layer: Semiconductive layer.

Earth Conductor: Split into two in the outer interstices.

Fiber Optics: FO 50/125 or 62.5/125 or E9/125μm within protection sheath.

Inner Sheath: EPR.

Outer Sheath: CM.

»  Dimensions and Weight

3.6/6 kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No� ×mm² | mm | mm | kg/km |
| 3×25+2×25/2+1×(6LWL) | 40�1 | 43�1 | 2650 |
| 3×25+2×50/2+1×(6LWL) | 42�4 | 45�4 | 3060 |
| 3×35+2×25/2+1×(6LWL) | 42�3 | 45�3 | 3060 |
| 3×35+2×50/2+1×(6LWL) | 44�0 | 47�0 | 3410 |
| 3×50+2×25/2+1×(6LWL) | 43�8 | 46�8 | 3490 |
| 3×50+2×50/2+1×(6LWL) | 46�1 | 49�1 | 3640 |
| 3×70+2×35/2+1×(6LWL) | 47�0 | 50�0 | 4350 |
| 3×70+2×50/2+1×(6LWL) | 52�0 | 56�0 | 5280 |
| 3×95+2×50/2+1×(6LWL) | 52�2 | 56�2 | 5550 |
| 3×120+2×70/2+1×(6LWL) | 49�6 | 50�9 | 7040 |
| 3×150+2×70/2+1×(6LWL) | 48�4 | 52�3 | 8000 |
| 3×185+2×95/2+1×(6LWL) | 51�3 | 55�3 | 9310 |
| 3×240+2×120/2+1×(6LWL) | 58�0 | 62�0 | 11940 |
| 3×300+2×150/2+1×(6LWL) | 63�2 | 67�2 | 14230 |

6/10 kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+2×25/2+1×(6LWL) | 41�4 | 44�4 | 2770 |
| 3×25+2×50/2+1×(6LWL) | 43�1 | 46�1 | 3120 |
| 3×35+2×25/2+1×(6LWL) | 43�6 | 46�6 | 3190 |
| 3×35+2×50/2+1×(6LWL) | 44�7 | 47�7 | 3470 |
| 3×50+2×25/2+1×(6LWL) | 45�1 | 48�1 | 3620 |
| 3×50+2×50/2+1×(6LWL) | 46�8 | 49�8 | 4010 |
| 3×70+2×35/2+1×(6LWL) | 48�3 | 51�3 | 4500 |
| 3×70+2×50/2+1×(6LWL) | 52�7 | 56�7 | 5360 |
| 3×95+2×50/2+1×(6LWL) | 53�5 | 57�5 | 5710 |
| 3×120+2×70/2+1×(6LWL) | 57�2 | 61�2 | 6830 |
| 3×150+2×70/2+1×(6LWL) | 62�3 | 66�3 | 8180 |
| 3×185+2×95/2+1×(6LWL) | 65�3 | 69�3 | 9500 |
| 3×240+2×120/2+1×(6LWL) | 73�4 | 77�4 | 12160 |
| 3×300+2×150/2+1×(6LWL) | 78�6 | 82�6 | 14460 |

8.7/15 kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+2×25/2+1×(6LWL) | 44�2 | 47�2 | 3050 |
| 3×25+2×50/2+1×(6LWL) | 45�4 | 48�4 | 3350 |
| 3×35+2×25/2+1×(6LWL) | 45�3 | 48�3 | 3320 |
| 3×35+2×50/2+1×(6LWL) | 47�0 | 50�0 | 3710 |
| 3×50+2×25/2+1×(6LWL) | 49�4 | 53�4 | 4160 |
| 3×50+2×50/2+1×(6LWL) | 51�2 | 55�2 | 4590 |
| 3×70+2×35/2+1×(6LWL) | 52�7 | 56�7 | 5080 |
| 3×70+2×50/2+1×(6LWL) | 55�0 | 59�0 | 5640 |
| 3×95+2×50/2+1×(6LWL) | 57�0 | 61�0 | 6160 |
| 3×120+2×70/2+1×(6LWL) | 62�1 | 66�1 | 7520 |
| 3×150+2×70/2+1×(6LWL) | 65�7 | 69�7 | 8670 |
| 3×185+2×95/2+1×(6LWL) | 68�7 | 72�7 | 10010 |
| 3×240+2×120/2+1×(6LWL) | 76�8 | 80�8 | 12730 |
| 3×300+2×150/2+1×(6LWL) | 82�0 | 86�0 | 15080 |

12/20 kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+2×25/2+1×(6LWL) | 45�5 | 48�5 | 3140 |
| 3×25+2×50/2+1×(6LWL) | 47�2 | 50�2 | 3530 |
| 3×35+2×25/2+1×(6LWL) | 48�3 | 51�3 | 3640 |
| 3×35+2×50/2+1×(6LWL) | 51�0 | 55�0 | 4240 |
| 3×50+2×25/2+1×(6LWL) | 52�5 | 56�5 | 4530 |
| 3×50+2×50/2+1×(6LWL) | 52�5 | 56�5 | 4690 |
| 3×70+2×35/2+1×(6LWL) | 55�7 | 59�7 | 5460 |
| 3×70+2×50/2+1×(6LWL) | 58�0 | 62�0 | 6040 |
| 3×95+2×50/2+1×(6LWL) | 61�4 | 65�4 | 6770 |
| 3×120+2×70/2+1×(6LWL) | 65�1 | 69�1 | 7950 |
| 3×150+2×70/2+1×(6LWL) | 68�7 | 72�7 | 9130 |
| 3×185+2×95/2+1×(6LWL) | 73�2 | 77�2 | 10770 |
| 3×240+2×120/2+1×(6LWL) | 79�8 | 83�8 | 13260 |
| 3×300+2×150/2+1×(6LWL) | 86�3 | 91�3 | 16040 |

14/25 kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+2×25/2+1×(6LWL) | 50�3 | 54�3 | 3740 |
| 3×25+2×50/2+1×(6LWL) | 50�3 | 54�3 | 3900 |

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×35+2×25/2+1×(6LWL) | 53�1 | 57�1 | 4270 |
| 3×35+2×50/2+1×(6LWL) | 53�1 | 57�1 | 4440 |
| 3×50+2×25/2+1×(6LWL) | 56�3 | 60�3 | 5000 |
| 3×50+2×50/2+1×(6LWL) | 56�3 | 60�3 | 5160 |
| 3×70+2×35/2+1×(6LWL) | 61�0 | 65�0 | 6190 |
| 3×70+2×50/2+1×(6LWL) | 61�0 | 65�0 | 6390 |
| 3×95+2×50/2+1×(6LWL) | 65�3 | 69�3 | 7340 |
| 3×120+2×70/2+1×(6LWL) | 69�0 | 73�0 | 8550 |
| 3×150+2×70/2+1×(6LWL) | 74�0 | 78�0 | 10020 |
| 3×185+2×95/2+1×(6LWL) | 77�0 | 81�0 | 11410 |
| 3×240+2×120/2+1×(6LWL) | 85�0 | 90�0 | 14380 |
| 3×300+2×150/2+1×(6LWL) | 90�2 | 95�2 | 16820 |

18/30 kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+2×25/2+1×(6LWL) | 53�7 | 57�7 | 4140 |
| 3×25+2×50/2+1×(6LWL) | 53�7 | 57�7 | 4310 |
| 3×35+2×25/2+1×(6LWL) | 56�6 | 60�6 | 4720 |
| 3×35+2×50/2+1×(6LWL) | 56�6 | 60�6 | 4880 |
| 3×50+2×25/2+1×(6LWL) | 61�2 | 65�2 | 5680 |
| 3×50+2×50/2+1×(6LWL) | 61�2 | 65�2 | 5840 |
| 3×70+2×35/2+1×(6LWL) | 64�4 | 68�4 | 6670 |
| 3×70+2×50/2+1×(6LWL) | 64�4 | 68�4 | 6870 |
| 3×95+2×50/2+1×(6LWL) | 68�7 | 72�7 | 7860 |
| 3×120+2×70/2+1×(6LWL) | 73�8 | 77�8 | 9350 |
| 3×150+2×70/2+1×(6LWL) | 77�5 | 81�5 | 10630 |
| 3×185+2×95/2+1×(6LWL) | 80�5 | 84�5 | 12040 |
| 3×240+2×120/2+1×(6LWL) | 88�5 | 93�5 | 15070 |
| 3×300+2×150/2+1×(6LWL) | 94�7 | 99�7 | 17780 |