NTSCGEWOEU Flexible Medium Voltage Trailing Cable

»  Applications

These cables are used as power supply or connection cables for large material handling machines,

e.g. excavators in open-cast mines subject to extremely high mechanical stresses. Particularly suitable

for applications in which abrasion and chaffing stresses are to be expected in trailing operation.

»  Standards

VDE 0250 Part 813

»  Construction

Stranded Copper Conductor 3GI3 Rubber Insulation Reinforcing Tape

5GM5 Rubber Inner Sheath Earth Conductor

5GM5 Rubber Outer Sheath

Conductors: Flexible stranded tinned copper conductor, class 5 according to DIN VDE 0295.

Inner Conductor Layer: Semiconductive layer.

Insulation: Rubber type 3GI3.

Outer Conductor Layer: Semiconductive layer.

Earth Conductor: Split into three in the outer interstices or Individual concentric distributed over core insulating coverings (coding…../3E).

Reinforcing Tape: Extremely tear-resistant reinforcing tape.

Inner Sheath: Rubber type 5GM5, abrasion and tear resistant, oil and ozone resistant.

Outer Sheath: Rubber type 5GM5, abrasion and tear resistant, oil and ozone resistant, inseparably bonded with inner sheath.

»  Dimensions and Weight

1.8/3kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+3×25/3 | 38�5 | 41�5 | 2470 |
| 3×35+3×25/3 | 42�9 | 45�9 | 3080 |
| 3×50+3×25/3 | 46�1 | 49�1 | 3750 |
| 3×70+3×35/3 | 49�7 | 53�7 | 4690 |
| 3×95+3×50/3 | 57�4 | 61�4 | 6210 |
| 3×120+3×70/3 | 61�2 | 65�2 | 7430 |
| 3×150+3×70/3 | 66�7 | 70�7 | 8900 |
| 3×185+3×95/3 | 70�6 | 74�6 | 10330 |
| 3×25+2×25/2+1×10ST | 40�3 | 44�3 | 2470 |
| 3×35+2×25/2+1×10ST | 42�9 | 46�9 | 3080 |
| 3×50+2×25/2+1×10ST | 46�8 | 50�8 | 3750 |
| 3×70+2×35/2+1×10ST | 51�5 | 55�5 | 4690 |
| 3×95+2×50/2+1×10ST | 57�4 | 62�4 | 6210 |
| 3×120+2×70/2+1×10ST | 63�6 | 68�6 | 7430 |
| 3×150+2×70/2+1×10ST | 67�2 | 72�2 | 8900 |
| 3×185+2×95/2+1×10ST | 70�2 | 75�2 | 10330 |

3.6/6kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+3×25/3 | 44�6 | 47�6 | 3080 |
| 3×35+3×25/3 | 47�6 | 50�6 | 3590 |
| 3×50+3×25/3 | 52�4 | 56�4 | 4520 |
| 3×70+3×35/3 | 56�3 | 60�3 | 5520 |
| 3×95+3×50/3 | 59�9 | 63�9 | 6580 |
| 3×120+3×70/3 | 65�6 | 69�6 | 8110 |
| 3×150+3×70/3 | 69�3 | 73�3 | 9320 |
| 3×185+3×95/3 | 73�2 | 77�2 | 10780 |
| 3×25+2×25/2+1×10ST | 45�0 | 49�0 | 3200 |
| 3×35+2×25/2+1×10ST | 47�6 | 51�6 | 3680 |
| 3×50+2×25/2+1×10ST | 53�0 | 57�0 | 4640 |
| 3×70+2×35/2+1×10ST | 56�2 | 60�2 | 5550 |
| 3×95+2×50/2+1×10ST | 61�8 | 66�8 | 6650 |
| 3×120+2×70/2+1×10ST | 66�1 | 71�1 | 8160 |
| 3×150+2×70/2+1×10ST | 69�8 | 74�8 | 9340 |
| 3×185+2×95/2+1×10ST | 74�6 | 79�6 | 10890 |

6/10 kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+3×25/3 | 46�4 | 49�4 | 3270 |
| 3×35+3×25/3 | 49�1 | 53�1 | 3800 |
| 3×50+3×25/3 | 54�1 | 58�1 | 4750 |
| 3×70+3×35/3 | 58�0 | 62�0 | 5750 |
| 3×95+3×50/3 | 61�7 | 65�7 | 6830 |
| 3×120+3×70/3 | 67�4 | 71�4 | 8380 |
| 3×150+3×70/3 | 71�0 | 75�0 | 9620 |
| 3×185+3×95/3 | 76�7 | 80�7 | 11430 |
| 3×25+2×25/2+1×10ST | 46�8 | 50�8 | 3410 |
| 3×35+2×25/2+1×10ST | 50�9 | 54�9 | 3890 |
| 3×50+2×25/2+1×10ST | 54�5 | 58�9 | 4860 |
| 3×70+2×35/2+1×10ST | 58�0 | 62�0 | 5780 |
| 3×95+2×50/2+1×10ST | 63�5 | 68�5 | 6920 |
| 3×120+2×70/2+1×10ST | 67�8 | 72�8 | 8450 |
| 3×150+2×70/2+1×10ST | 71�5 | 76�5 | 9620 |
| 3×185+2×95/2+1×10ST | 76�3 | 81�3 | 10980 |

8.7/15 kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+3×25/3 | 52�6 | 56�6 | 4040 |
| 3×35+3×25/3 | 55�6 | 59�6 | 4630 |
| 3×50+3×25/3 | 58�9 | 62�9 | 5370 |
| 3×70+3×35/3 | 64�5 | 68�5 | 6720 |
| 3×95+3×50/3 | 68�2 | 72�2 | 7850 |
| 3×120+3×70/3 | 72�1 | 76�1 | 9130 |
| 3×150+3×70/3 | 77�6 | 81�6 | 10750 |
| 3×185+3×95/3 | 81�5 | 85�5 | 12290 |
| 3×25+2×25/2+1×10ST | 53�0 | 57�0 | 4130 |
| 3×35+2×25/2+1×10ST | 55�6 | 59�6 | 4740 |
| 3×50+2×25/2+1×10ST | 59�3 | 63�3 | 5470 |
| 3×70+2×35/2+1×10ST | 64�6 | 68�6 | 6820 |
| 3×95+2×50/2+1×10ST | 68�3 | 73�3 | 7950 |
| 3×120+2×70/2+1×10ST | 74�4 | 79�4 | 9240 |
| 3×150+2×70/2+1×10ST | 78�1 | 83�1 | 10860 |
| 3×185+2×95/2+1×10ST | 81�1 | 86�1 | 12400 |

12/20 kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+3×25/3 | 56�9 | 60�9 | 4620 |
| 3×35+3×25/3 | 59�9 | 63�9 | 5220 |
| 3×50+3×25/3 | 65�0 | 69�0 | 6300 |
| 3×70+3×35/3 | 68�9 | 72�9 | 7410 |
| 3×95+3×50/3 | 72�5 | 76�5 | 8560 |
| 3×120+3×70/3 | 78�2 | 82�2 | 10260 |
| 3×150+3×70/3 | 81�9 | 85�9 | 11570 |
| 3×185+3×95/3 | 87�4 | 92�4 | 13530 |
| 3×25+2×25/2+1×10ST | 57�3 | 61�3 | 4770 |
| 3×35+2×25/2+1×10ST | 59�9 | 63�9 | 5340 |
| 3×50+2×25/2+1×10ST | 65�4 | 69�4 | 6460 |
| 3×70+2×35/2+1×10ST | 68�8 | 72�8 | 7450 |
| 3×95+2×50/2+1×10ST | 74�4 | 79�4 | 8680 |
| 3×120+2×70/2+1×10ST | 78�7 | 83�7 | 10370 |
| 3×150+2×70/2+1×10ST | 82�2 | 87�2 | 11650 |
| 3×185+2×95/2+1×10ST | 87�0 | 92�0 | 13090 |

14/25kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+2×25/2+1×10ST | 64�7 | 68�7 | 5940 |
| 3×35+2×25/2+1×10ST | 67�3 | 71�3 | 6470 |
| 3×50+2×25/2+1×10ST | 71�0 | 75�0 | 7300 |
| 3×70+2×35/2+1×10ST | 75�2 | 80�2 | 8800 |
| 3×95+2×50/2+1×10ST | 80�0 | 85�0 | 10050 |
| 3×120+2×70/2+1×10ST | 85�9 | 90�9 | 11470 |
| 3×150+2×70/2+1×10ST | 89�6 | 94�6 | 13210 |
| 3×185+2×95/2+1×10ST | 92�6 | 97�6 | 14860 |

18/30kV

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×25+3×25/3 | 69�5 | 73�5 | 6680 |
| 3×35+3×25/3 | 72�5 | 76�5 | 7380 |
| 3×50+3×25/3 | 77�6 | 81�6 | 8460 |
| 3×70+3×35/3 | 81�5 | 85�5 | 9690 |
| 3×95+3×50/3 | 84�9 | 89�9 | 10960 |
| 3×120+3×70/3 | 90�6 | 95�6 | 12830 |

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×150+3×70/3 | 94�3 | 99�3 | 14250 |
| 3×185+3×95/3 | 100�0 | 105�0 | 16390 |
| 3×25+2×25/2+1×10ST | 69�9 | 73�9 | 7100 |
| 3×35+2×25/2+1×10ST | 72�6 | 76�6 | 7540 |
| 3×50+2×25/2+1×10ST | 78�0 | 82�0 | 8680 |
| 3×70+2×35/2+1×10ST | 80�4 | 85�4 | 9760 |
| 3×95+2×50/2+1×10ST | 86�8 | 91�8 | 11100 |
| 3×120+2×70/2+1×10ST | 91�1 | 96�1 | 12980 |
| 3×150+2×70/2+1×10ST | 94�8 | 99�8 | 14350 |
| 3×185+2×95/2+1×10ST | 99�6 | 104�6 | 15870 |