Caledonian Mining Cables Cables for Underground Mining

NSSHCGEOEU 0.6/1kV Coal Cutter Cable (Low Tensile Stress)

»  Applications

These cables are used for the connection of mobile machines under extremely high mechanical loads, predominantly in mining situations, e.g. for coal-cutting machines, suitable for extreme bending loads under low tensile stress.

»  Standards

DIN VDE 0250 Part 812

»  Construction

3GI3 Rubber Insulation

Stranded Tinned Copper Conductor Monitoring Conductor

Outer Conductor Layer

GM1b Rubber Inner Sheath Spiral Of Copper And Steel Wires Pilot Cores

5GM5 Rubber Outer Sheath

Conductors: Flexible stranded tinned copper conductor.

Insulation: Heat resistant 3GI3 rubber based on EPR.

Outer Conductor Layer: Easy strippable outer conductive layer.

Pilot Cores: Copper strand and steel braid conductor capable of expansion and compression with EPR rubber insulation.

Monitoring Cores: Spiral of tinned copper wires above the pilot cores, covered with a semi- conductive tape.

Inner Sheath: Rubber type GM1b.

Armour/Earth Conductor: Concentric earth conductor as spiral of copper and steel wires,

fibreglas tape, embedded in the outer sheath which prevents sheath exchanging.

Outer Sheath: Rubber type 5GM5, abrasion and tear resistant, oil resistant and flame retardant.

www.caledonian-cables.co.uk  www.addison-cables.com	17

Caledonian Mining Cables

Cables for Underground Mining

»  Dimensions and Weight

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×16/16KON+2ST+UEL | 35�0 | 38�0 | 2130 |
| 3×25/16KON+2ST+UEL | 38�0 | 41�0 | 2790 |
| 3×35/16KON+2ST+UEL | 41�0 | 45�0 | 3390 |
| 3×50/25KON+2ST+UEL | 47�0 | 51�0 | 4340 |
| 3×70/35KON+2ST+UEL | 52�0 | 56�0 | 5680 |
| 3×95/50KON+2ST+UEL | 58�0 | 62�0 | 7180 |
| 3×25/16KON+3×(1.5ST+UEL) | 38�0 | 41�0 | 2920 |
| 3×35/16KON+3×(1.5ST+UEL) | 41�0 | 45�0 | 3630 |
| 3×50/25KON+3×(1.5ST+UEL) | 45�0 | 48�0 | 4500 |
| 3×70/35KON+3×(1.5ST+UEL) | 48�0 | 53�0 | 5850 |
| 3×95/50KON+3×(1.5ST+UEL) | 52�0 | 56�0 | 7400 |
| 3×120/70KON+3×(1.5ST+UEL) | 58�0 | 63�0 | 8300 |
| 3×150/70KON+3×(1.5ST+UEL) | 62�0 | 68�0 | 9300 |

18	www.caledonian-cables.co.uk  www.addison-cables.com