Caledonian Mining Cables Cables for Underground Mining

NSSHOEU-O/J 0.6/1kV Heavy Duty Flexible Cable

»  Applications

These cables are designed for the connection of mobile equipment and machines under very high mechanical loads in dry and damp areas, outdoors and in explosion hazard areas, particularly in mining and industry, quarries and building sites.

»  Standards

VDE 0250 Part 812

»  Construction

Stranded Tinned Copper Conductor 3GI3 Rubber Insulation GM1b/5GM3 Rubber Inner Sheath 5GM5 Rubber Outer Sheath

Conductors: Flexible stranded tinned copper conductor, class 5 according to DIN VDE 0295.

Insulation: Heat resistant EPR type 3GI3.

Inner Sheath: SR/SBR/PCP/CR type GM1b/5GM3.

Outer Sheath: Chlorinated rubber PCP/CR type 5GM5, abrasion and tear resistant, oil resistant

and flame retardant.

»  Dimensions and Weight

NSSHOEU-O

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 1×16 | 11�0 | 13�0�5�0 | 260 |
| 1×25 | 13�0 | 16�0 | 390 |
| 1×35 | 14�0 | 17�0 | 500 |

www.caledonian-cables.co.uk  www.addison-cables.com	21

Caledonian Mining Cables

Cables for Underground Mining

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 1×50 | 16�0 | 19�0 | 680 |
| 1×70 | 18�0 | 21�0 | 900 |
| 1×95 | 20�0 | 24�0 | 1150 |
| 1×120 | 23�0 | 27�0 | 1440 |
| 1×150 | 24�0 | 28�0 | 1750 |
| 1×185 | 28�0 | 31�0 | 2300 |
| 1×240 | 32�0 | 36�0 | 3000 |
| 2×1�5 | 11�0 | 14�0 | 210 |
| 3×2�5 | 13�0 | 16�0 | 300 |

NSSHOEU-J

| Number of Cores×Nominal Cross Section | Minimium Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. ×mm² | mm | mm | kg/km |
| 3×1�5 | 12�0 | 15�0 | 240 |
| 3×70/35 | 46�0 | 51�0 | 4450 |
| 3×95/50 | 54�0 | 59�0 | 5870 |
| 3×120/70 | 59�0 | 64�0 | 7340 |
| 4×1�5 | 13�0 | 16�0 | 280 |
| 4×2�5 | 15�0 | 18�0 | 400 |
| 4×4 | 17�0 | 20�0 | 510 |
| 4×6 | 18�0 | 21�0 | 630 |
| 4×10 | 22�0 | 26�0 | 950 |
| 4×16 | 28�0 | 32�0 | 1430 |
| 4×25 | 33�0 | 37�0 | 2100 |
| 4×35 | 36�0 | 40�0 | 2650 |
| 4×50 | 42�0 | 47�0 | 3660 |
| 5×1�5 | 13�0 | 16�0 | 320 |
| 5×2�5 | 16�0 | 19�0 | 470 |
| 5×4 | 18�0 | 21�0 | 600 |
| 5×6 | 20�0 | 24�0 | 780 |
| 5×10 | 24�0 | 28�0 | 1130 |
| 5×16 | 29�0 | 34�0 | 1720 |
| 5×25 | 35�0 | 39�0 | 2470 |
| 6×2�5 | 13�0 | 16�0 | 300 |
| 7×1�5 | 16�0 | 19�0 | 470 |
| 7×2�5 | 18�0 | 21�0 | 600 |
| 10×1�5 | 19�0 | 22�0 | 570 |
| 10×2�5 | 21�0 | 25�0 | 790 |
| 12×2�5 | 22�0 | 26�0 | 860 |
| 18×2�5 | 28�0 | 32�0 | 1240 |

22	www.caledonian-cables.co.uk  www.addison-cables.com